## Slide 1
INTRODUCTION 1
High-pressure physics and strongly-correlated materials
Simplified phase diagram of solid oxygen
T (K)
P (GPa)
10
96
RT
Fmmm
(O2)4
C2h(C2/m)
C2h(C2/m)
The Hubbard- and van der Waals-corrections on the DFT calculations of the epsilon-zeta transition in the solid oxygen
Le The Anh
Quemix Inc.
INTRODUCTION 2
Experimental methods to explore the structures
Yuichi Akahama et al 2019 Jpn. J. Appl. Phys. 58 095502
X-Ray diffraction
Raman
IR absorption
INTRODUCTION 3
Theoretical physics of many-body systems
1. Hartree-Fock
2. Hubbard V
3. van-der-Waals
Semi-empirical
Fully ab-initio
+U vs +U+vdW: Structure
Phys. Chem. Chem. Phys., 2023,25, 25654-25658
PBE+U
PBE+U+vdW-D
vdW-DF+U
Phys. Chem. Chem. Phys., 2023,25, 25654-25658
Metallization vs Structural transition
Hartree-Fock physics
J. Chem. Theory Comput. 2015, 11, 3, 1195–1205
B3LYP also predicted the co-existence of the epsilon and zeta phases.
Un-solved problems
Jpn. J. Appl. Phys. 2019 58, 095502
Zeta phase: Pm symmetry has lower enthalpy than C2/m
PRB 2024 110, 064106
C2h(C2/m): 12 Raman + 9 IR
D2h: 9 Raman + 6 IR
DFT
Exp.
Summary
High pressure phases of solid oxygen are complex.
It requires both correct short-range and long-range treatments on the equal footing.
Summary
Possible long-range treatments are:
  Hartree-Fock exchange
  Inter-site Hubbard +V
  van-der-Waals
Within the two-body correlation approximation.